## Slide 1: Determination of Oxygen Local Bonding in Lithium Transition Metal Oxides using Computed XANES: A Machine Learning Approach
Liang Li
09/12/2018 subgroup meeting

## Slide 2
A great tool to probe local geometries/electronic states
http://www.laboratory-journal.com/
Advanced Photon Source @ Argonne
C.L. Dong et al. 2007 SPIE Newsroom
X-Ray Absorption Spectroscopy (XAS): probe the unoccupied states that are filled by excited electrons
X-Ray Absorption Spectroscopy

## Slide 3
element-specific, sensitive to chemical information
image courtesy: R. Sarangi
X-ray Absorption Near-Edge Structure

## Slide 4
Difficulty of Inverse Problem
Gerald Seidler, Machine Learning vs. XAFS Interpretation
Real-space multi-scattering, BSE, excited core-hole…
Machine learning

## Slide 5
Using ML to Determine Nanoparticle Structures
J. Timoshenko, J. Phys. Chem. Lett. 8, 5091-5098 (2017)
129 nodes in input layer
Two hidden layers, 339 – 387 nodes in each
Hyperbolic tangent function as activation function

## Slide 6
Oxygen Local Environments in Li3FeO3.5
Li
O
Fe
AIMD at 15 ps
AIMD at 20 ps
NFe = 0
NFe = 1
NFe = 2
NFe = 3
NFe = 4
Fe coordination is an indicator of relative Li concentration
Affects oxygen electronic structure and number of electrons for battery capacity
cutoff radius = 2.6 Å

## Slide 7
Li3FeO3.5
Li3FeO3.5 with peroxo O-O dimer
Li3FeO3.5 with superoxo O-O dimer
Simulated Oxygen XANES
Goal: Determine the number of Fe bound to oxygen based on calculated XANES
Multi-class classification problem
Three Li3FeO3.5 structures, 49 oxygen atoms in each
147 examples in total
Intensities in the energy range of 0-14 eV used as input. 170 data points for each spectrum.

## Slide 8
. . .
. . .
x1
x2
x3
.
.
.
x169
x170
NFe = 0
NFe = 1
NFe = 2
NFe = 3
NFe = 4
(170 x 147)
(5 x 147)
Neural Network Architecture (Multi-Class Classification)
input layer
hidden layer
output layer

## Slide 9
(1) =
(2) ()
-th unit of -th layer
Hidden layer activation function ():
Rectified Linear Units (ReLU)
or hyperbolic tangent function
: activation function
Neural Network Architecture (Multi-Class Classification)

## Slide 10
(1) =
(2) ()
Output layer activation function ():
Softmax function:
e.g.
Neural Network Architecture (Multi-Class Classification)

## Slide 11
Loss function:
(1) =
(2) ()
-th unit of -th layer
Neural Network Architecture (Multi-Class Classification)

## Slide 12
Number of hidden layers
Number of nodes in each hidden layer
Activation function of each hidden layer (ReLU or tanh)
Learning rate
With or without regularization
Optimization algorithm (Adam)
147 examples, 110 training, 37 test
TensorFlow
Hyperparameters to Tune

## Slide 13
Results
ReLU + ReLU |  | 
 | w/o regularization | w/ regularization
Train accuracy | 1.00 | 1.00
Test accuracy | 0.81 | 0.86
w/ regularization |  |  |  | 
 | ReLU + ReLU | tanh + tanh | Tanh + ReLU | ReLU + tanh
Train accuracy | 1.00 | 0.99 | 0.97 | 0.96
Test accuracy | 0.86 | 0.89 | 0.89 | 0.94
ReLU + ReLU
ReLU + tanh
14 nodes on first hidden layer
9 nodes on second hidden layer
5 nodes on output layer
overfitting

## Slide 14
Results
ReLU + tanh w/ regularization |  |  |  | 
 | 14 + 9 | 12+8 | 10+8 | 7+6
Train accuracy | 0.96 | 0.99 | 0.97 | 0.96
Test accuracy | 0.94 | 0.97 | 0.89 | 0.92
number of nodes in the hidden layer:

## Slide 15
Conclusions:
A three-layer neural network was constructed to predict the Fe coordination numbers around oxygen in Li transition metal oxide.
A training accuracy ~ 95% was achieved.
Similar NN architecture can be used in other Li-TM oxide systems.
More training examples would be desirable.